## Slide 1
Physical properties of solids
determined by electronic structure
related to movement of atoms
about their equilibrium positions
Sound velocity
Thermal properties: -specific heat
-thermal expansion
-thermal conductivity
(for semiconductors)
Hardness of perfect single crystals (without defects)
Lattice Dynamics

## Slide 2
Reminder to the physics of oscillations and waves:
Harmonic oscillator in classical mechanics:
Example: spring pendulum
Hooke’s law
x
Equation of motion:
or
where
Solution with
where
X=A sin ωt
X
Dx

## Slide 3
Traveling plane waves:
X
0
Y
X=0:
t=0:
Particular state of oscillation Y=const
in particular
or
travels according
solves wave equation

## Slide 4
Transverse wave
Longitudinal wave
Standing wave

## Slide 5
Large wavelength λ
Crystal can be viewed as a continuous medium:
good for
λ>10-8m
10-10m
Speed of longitudinal wave:
where Bs: bulk modulus
with
compressibility
Bs determines elastic deformation energy density
dilation
(ignoring anisotropy of the crystal)
E.g.: Steel
Bs=160 109N/m2
ρ=7860kg/m3
(click for details in thermodynamic context)

## Slide 6
>> interatomic spacing
continuum approach fails
In addition:
phonons
vibrational modes quantized

## Slide 7
Linear chain:
Remember: two coupled harmonic oscillators
Superposition of normal modes
Symmetric mode
Anti-symmetric mode
Vibrational Modes of a Monatomic Lattice

## Slide 8
generalization
Infinite linear chain
How to derive the equation of motion in the harmonic approximation
?
n
n+1
n+2
n-1
n-2
un
un+1
un+2
un-1
un-2
un
un+1
un+2
un-1
un-2
fixed
D
a

## Slide 9
Total force driving atom n back to equilibrium
n
n
equation of motion
Solution of continuous wave equation
approach for linear chain
,
,
?
Let us try!
Alternative without thinking
Lagrange formalism

## Slide 10
Continuum limit of acoustic waves:
k
Note: here pictures of transversal waves
although calculation for the longitudinal case

## Slide 11
k
, here h=1
1-dim. reciprocal
lattice vector Gh
Region
is called
first Brillouin zone

## Slide 12
We saw: all required information contained in a particular volume in reciprocal space
first Brillouin zone
1d:
a
where m=hn integer
1st Brillouin zone
In general: first Brillouin zone
Wigner-Seitz cell of the reciprocal lattice
Brillouin zones

## Slide 14
Vibrational Spectrum for structures with 2 or more atoms/primitive basis
Linear diatomic chain:
2n
2n+1
2n+2
2n-1
2n-2
u2n
u2n+1
u2n+2
u2n-1
u2n-2
D
a
2a
Equation of motion for atoms on even positions:
Equation of motion for atoms on even positions:
Solution with:
and

## Slide 15
,
2
2
Click on the picture to start the animation M->m
note wrong axis in the movie

## Slide 16
Atomic Displacement
Optic Mode
Atomic Displacement
Acoustic Mode
Click for animations

## Slide 17
Dispersion curves of 3D crystals
Every additional atom of the primitive basis
3D crystal: clear separation into longitudinal and transverse mode only possible in
particular symmetry directions
Every crystal has 3 acoustic branches
sound waves
of elastic theory
1 longitudinal
2 transverse
acoustic
further 3 optical branches
again 2 transvers
1 longitudinal
p atoms/primitive unit cell ( primitive basis of p atoms):
3 acoustic branches
+ 3(p-1) optical branches
= 3p branches
1LA +2TA
(p-1)LO +2(p-1)TO

## Slide 18
Intuitive picture:
1atom
3 translational degrees of freedom
3+3=6 degrees of freedom=3 translations+2rotations
+1vibraton
Solid: p N atoms
no translations, no rotations
3p N vibrations
x
y
z
# of primitive
unit cells
# atoms
in primitive
basis

## Slide 19
diamond lattice: fcc lattice with basis
(0,0,0)
Longitudinal Acoustic
Longitudinal Optical
Transversal Acoustic
degenerated
Part of the phonon dispersion relation of diamond
Transversal Optical
degenerated
P=2
2x3=6 branches expected
2 fcc sublattices vibrate against one another
However, identical atoms
no dipole moment

## Slide 20
Calculated phonon dispersion relation
of Ge (diamond structure)
Calculated phonon dispersion relation
of GaAs (zincblende structure)
Adapted from:
H. Montgomery, “ The symmetry of lattice vibrations in zincblende and diamond structures”, Proc. Roy. Soc. A. 309, 521-549 (1969)

## Slide 21
Inelastic interaction of light and particle waves with phonons
Constrains: conservation law of
momentum
energy
Condition for
elastic
scattering
in
± q
incoming wave
scattered wave
Reciprocal lattice
vector
phonon
wave
vector
elastic
sattering
in
“quasimomentum”
for neutrons
for photon
scattering
Phonon spectroscopy

## Slide 23
Triple axis neutron spectrometer
@ ILL in Grenoble, France

## Slide 24
Lonely scientist in the reactor hall
Very expensive and involved experiments
Table top alternatives
?
Yes, infra-red absorption and
inelastic light scattering (Raman and Brillouin)
However only
accessible
see homework #8