## Slide 1
Ionic Bond
electrostatic interaction of oppositely charged ions
Example: NaCl (sodium chloride)
positive and negative ions arrange by:
Coulomb attraction:
between ions of opposite sign
Coulomb repulsion:
between ions of same sign
Repulsion more than compensated by attraction
Ionic bond

## Slide 2
6.1 eV
(electrostatic energy)
∞
5.1 eV
(ionization energy)
3.6 eV
(electron affinity)
Closer look to energetic
Na+
+
∞
+
Cl
+
Cl-
+
Na+
+
Cl-
Cl-
Na+
r0
+
-0.3 eV (Pauli repulsion)

## Slide 3
Click for reference and additional
information
Cl
+
Cl-
Na+
r0
+
4.3 eV=
(6.1-0.3)eV-5.1eV+3.6eV
(dissociation energy)
How to find r0
?
minimum

## Slide 4
From a single Na+Cl- bond to the NaCl solid
Neither contact between cations (Na+ ) nor contact between anions (Cl- )
apart from nearest-neighbor interaction only Coulomb terms involved
r0

## Slide 5
Na+ has:
6 Cl- nearest neighbors at distance r0
12 Na+ next nearest neighbors at
r0
8 Cl- further neighbors at distance

## Slide 6
Total Coulomb energy per ion pair: Ecoul
Ecoul= E( 6 Cl- nearest neighbors at distance r0 ) + E( 12 Na+ nearest neighbors at distance )
+ E( 8 Cl- at distance )+…
where α=1.748 is the Madelung constant
Erwin Rudolf Madelung
1881-1972
Series
alternating sign
slow convergence
methods for accurate sums
Ewald (1921) and Evjen (1932)
Madelung Constants
Notes: Madelung Constants
Compound
Crystal Lattice
M
NaClNaCl1.74756CsClCsCl1.76267CaF2Cubic2.51939CdCl2Hexagonal2.244MgF2Tetragonal2.381ZnS (wurtzite)Hexagonal1.64132TiO2 (rutile)Tetragonal2.408bSiO2 Hexagonal2.2197Al2O3Rhombohedral4.1719

## Slide 7
Compound | Crystal Lattice | M
NaCl | NaCl | 1.74756
CsCl | CsCl | 1.76267
CaF2 | Cubic | 2.51939
CdCl2 | Hexagonal | 2.244
MgF2 | Tetragonal | 2.381
ZnS (wurtzite) | Hexagonal | 1.64132
TiO2 (rutile) | Tetragonal | 2.408
bSiO2 | Hexagonal | 2.2197
Al2O3 | Rhombohedral | 4.1719
Madelung Constants
(Data from Handbook Menu )

## Slide 8
unknown parameters
Total energy per ion pair: Ei=ECoul+ERepulsive
However: condition
r=r0
determination of,e.g., C

## Slide 9
Ei @ r=r0
Input from
experiment
bulk compressibility
since NaCl cubic
r
corner shared amog 8 adjacent cubes
1/8 (4Na+ +4Cl-)=1/2 NaCl
+
1 NaCl-molecule requires
Click here for response functions in gases.
Note that the bulk modulus B is inverse proportional to the bulk compressibility 

## Slide 10
work W=pdV related volume change
Let´s remember
Click for details. Note special sign convention in thermodynamics
Aim:
and

## Slide 11
Cohesive energie
Properties of ionic crystals
Mott and Gurney 1948
for all alkali halides
However: widely varying values of C in the repulsive term
?
(alkali)+
(halogen)-
closed-shell ions behave like incompressible spheres
take into account different radii according
universal C´ for all alkali halides
(can be experimentally determined via Born-Haber cycle)
Click for detailed information

## Slide 12: Ionic Sizes

## Slide 13
Completely ionic bond is an ideal case
In general bond neither covalent nore pure ionic
Mixed ionic-covalent bonds
determined from
Min.
Paulings concept of electronegativity
Electronegativity refers to the ability of an atom in a molecule to attract shared electrons.
Semi-quantitative estimation of λ
A
B
A
B
δ+
δ-
+

## Slide 14
>
E( )
A
A
E( )
B
B
]
1/2
[
A
B
δ+
δ-
E( )
because there is Coulomb interaction between δ+und δ-
empirical formula
better than
Linus Pauling
is the only person ever to receive two unshared Nobel Prizes
—for Chemistry (1954) and for Peace (1962).

## Slide 15
Find here Pauling’s electronegativity
online

## Slide 16
% ionicity of bond
determined from dipole moment of molecules
% ionicity of bond